## Slide 1: WEAR MECHANISM OF HIPIMS Mo-W DOPED CARBON COATINGS IN DRY AND BOUNDARY LUBRICATION CONDITIONS Papken Eh. Hovsepian 1), Paranjayee Mandal, 1) Arutiun P. Ehiasarian 1), G. Sáfrán 2), R. Tietema 3), D. Doerwald 3) 1)National HIPIMS Technology Centre, Materials and Engineering Research Institute, Sheffield Hallam University, Howard Street, Sheffield S1 1WB, UK, 2) Hungarian Academy of Sciences, Research Institute for Technical Physics and Materials Science, H-1121 Budapest, Konkoly-Thegeut 29-33 Hungary, 3) IHI Hauzer Techno Coating B.V. Van Heemskerckweg 22, 5928 LL Venlo, The Netherlands
National HIPIMS Technology Centre, UK

## Slide 2
100 % Carbon
100 % Metal
Diamond and DLC films: % Sp3 bonding
Me-doped DLC films: Me-type and content, % Sp3 bonding, H- content
Me-Carbon films: Me-type and content, graphitic- mainly Sp2 bonding, Coating Structure
Me- Carbide films: Me-type and Coating Structure
Me-Carbide + Me films: Me-type and Coating Structure
Me films
50 % Me
50 % C
Me-C Thin Films
Me-free DLC films: % Sp3 bonding, H- content
Utilisation of tribochemical reactions to achieve low friction and high wear resistance of Mo-W- C films in boundary lubrication and elevated temperature conditions. Application: automotive components
National HIPIMS Technology Centre, UK

## Slide 3: XSEM and TEM analyses of Mo-W doped Carbon films
National HIPIMS Technology Centre, UK

## Slide 4
a) Standard Ar-ion pre-treatment b) HIPIMS Me-ion pre-treatment
Amorphised interface with a more random structure Crystaline interface with well-defined orientation
Results in poor adhesion Results in strong adhesion EC, Innovatial Project
Image courtesy of Jeff Th.M. De Hosson, NMP3-CT-2005-515844
Department of Applied Physics,. Mater Scientific Centre, University of Groningen, The Netherlands
Interface structure after Ar- ion and Me - ion surface pre-treatment
National HIPIMS Technology Centre, UK

## Slide 5
National HIPIMS Technology Centre, UK
Adhesion of coating Mo-W-C deposited on HSS at 100N normal load
Lc=100N

## Slide 6
Friction behaviour of the Mo-W-C coatings after 7.5 km of dry sliding
National HIPIMS Technology Centre, UK

## Slide 7
Raman analyses of the wear track after dry sliding at room temperature
National HIPIMS Technology Centre, UK

## Slide 8: Crystal structure of MoO3 and WO3
National HIPIMS Technology Centre, UK

## Slide 9
Coefficient of friction of various DLC coatings compared to the Mo-W-C, (CMW1R) coating
Tests carried out with highly viscous Mobil1 Extended lifeTM 10W-60 multigrade synthetic engine oil free of friction modifiers
National HIPIMS Technology Centre, UK

## Slide 10
Raman analyses of the wear track after lubricated sliding at room temperature
Lubricant, 10W-60 engine oil
WS2 powder used as a standard
Wear track of Mo-W doped Carbon film
National HIPIMS Technology Centre, UK

## Slide 11
Raman analyses of the wear track after lubricated sliding at 200oC
WS2 powder used
as a standard
MoS2 powder used
as a standard
Different positions in the wear track of Mo-W doped Carbon film
National HIPIMS Technology Centre, UK

## Slide 12
National HIPIMS Technology Centre, UK

## Slide 13
Coefficient of friction of Mo-W-Carbon and DLC films as a function of sliding distance in lubricated sliding at 200oC against a 100Cr6 counterpart
National HIPIMS Technology Centre, UK

## Slide 14
Thermogravimetric analyses of various Me-doped C coatings and SOA DLC coating
National HIPIMS Technology Centre, UK

## Slide 15
Substrate exposed
Coating
Static oxidation behaviour of Me-C and DLC coatings
Me-C, 400oC
DLC, 400oC
Me-C, 500oC
DLC, 500oC
National HIPIMS Technology Centre, UK

## Slide 16
CONCLUSIONS
Me-doping of Carbon based films is a powerful tool for manipulation of coating structure, properties and therefore performance.
In dry sliding conditions the wear debris consisted of MoO3 and WO3 as well as debris of graphitic nature as indicated by the well pronounced D and G band in the Raman spectra. This is typical for oxidative wear mechanism.
In boundary lubrication condition, the friction behaviour of the Mo-W doped C coatings is dominated by the in situ formation of solid lubricants MoS2 and WS2 at the asperity contacts, which is typical for the tribochemical reaction wear mechanism.
Simultaneous doping of Carbon films with Mo and W is a key to maintain low coefficient of friction in wide temperature range . WS2 forms readily at low temperatures where as MoS2 contributes more effectively at higher temperatures.
Mo and W dopants provide effective tool for further enhancement of the high temperature stability of the Carbon based coatings.
The use of the HIPIMS technology brings further advantages as it provides conditions for deposition of highly adherent, very dense and smooth coatings.
Mo-W doped C coating solution is patent pending
National HIPIMS Technology Centre, UK